FIDDES LIQUID FLOOR WAX
PREPARATION	
Sand the wooden substrate in stages, working with a medium sandpaper (120 grit), through to a medium / fine grade (180 –220 grit). Always sand in the direction of the grain pattern where possible, ensuring the removal of any blemishes and glue residue prior to the application of Liquid Floor Wax. Take care to remove all traces of sanding dust. A coat of Fiddes Shellac Sealer or Clear Glaze is recommended on open grained wood flooring prior to application.
APPLICATION	
Take a clean cotton cloth and lightly apply in the direction of the wood grain where possible. To obtain a uniform coverage, always wipe evenly, taking care to lightly remove any excess Floor Wax immediately with a separate, clean absorbent cloth, again following the direction of the grain pattern.
Best results are achieved when Fiddes Floor Wax is applied sparingly, and worked in small areas at any one time. Buff to desired sheen level by hand or mechanical polisher. Clean applicators with White Spirit.
DRYING TIME	
10 – 15 minutes at room temperature
COVERAGE	
16 sqm per Litre (depending on substrate and method of application)
COATS	
1 coat
RECOMMENDED FOR USE ON	
Floors and surfaces of fine furniture and cabinet work.
PACKAGING	
1lt, 2lt, 5lt