W. S. Jenkins & Co. Ltd

Jeco Works, Tariff Road

Tottenham, London. N17 0EN

Tel: 020-8808 2336

Fax: 020-8365 1534

sales@wsjenkins.co.uk

# Jecofil

Description:	Thixotropic grain filler based on oil based resins, extenders and suitably coloured.

Uses:	To choke or fill the grain before polishing or lacquering to achieve a “full finish”

Colour range:	Transparent (neutral) J025, Medium Oak J026, Mahogany (light) J027, Walnut/Dark Oak J028, Light oak J029, Sapele J030, White (liming) J031, Dark (brown) Mahogany J080, Brown J086.

Drying Time:	Jecofil should preferably be left overnight to dry or a minimum of 4 hours.

Method:	Apply with coarse cloth i.e. Curtaining or Hessian in a circular motion, finishing off across the grain. Leave until the ‘wet look’ has gone then wipe off across the grain with a clean coarse cloth to remove the excess. Leave to dry overnight and paper with 150-180 grit sandpaper.

Finishing: 	Jecofil will except most stains and can be finished with most types of lacquers and polishes.

## Health & Safety: Consult label and COSHH data sheet prior to use.